## Slide 1: Reaction network (5wt% Pt/SBA-15 140C, 4h, 40Bar H2)
D-glucose
Conversion = 16.2%
D-fructose
Conversion = 21.1%
D-sorbitol
Conversion = 5.8%
D-mannitol
Conversion = Trace
Isomerization
Isomerization
+ H2
+ H2
+ H2
+ H2
Selectivity = 12.2%
Initial rate = 0.084 mmol/h
Initial rate = 0.041 mmol/h
Selectivity = 4.2%
Initial rate = 0.138 mmol/h
Selectivity = 28.5%
Trace
Selectivity = 9.9%
Initial rate = 0.072
mmol/h
Selectivity = 5.5%
Initial rate = 0.117 mmol/h
Selectivity = 11.4%
Initial rate = 0.021 mmol/h
Need to put rates of production or conversion on
for all steps.
X
HUMINS